Welded Connections

Calculation complies with SNiP II-23-81*

General Properties

Steel:

with design strength based on the ultimate strength Ru=369 N/mm2

with design strength based on the yield strength  Ry=246 N/mm2

| Importance factor | 1 |
| --- | --- |
| Service Factor | 1 |
| Group of structures according to table 50* SNiP II-23-81* | 4 |

| Properties of welding materials |
| --- |
| Characteristic strength of weld metal based on the ultimate strength, Rwun | 450 N/mm2 |
| Design shear strength of fillet welds, Rwf | 200 N/mm2 |
| Welding type | Manual |
| Position of weld | Flat |
| Climatic region | with temperature t > -40°C |

| Type | Properties |
| --- | --- |
|  | Weld leg = 8 mm b = 200 mm h = 250 mm t = 20 mm tf = 24 mm |

Results of analysis by load case combinations

|  | N | My | Qz |
| --- | --- | --- | --- |
|  | kN | kN*m | kN |
| 1 | 0 | 51 | 0 |

| Checked according to SNiP | Check | Utilization Factor |
| --- | --- | --- |
| Sec. 11.2 Formula (120) | Of the weld metal | 0,793 |
| Sec. 11.2 Formula (121) | Of the metal of the fusion border | 0,66 |

Utilization Factor 0,793 - Of the weld metal

Utilization factor over whole package of combinations 0,793 - Of the weld metal

Interaction Curves

| Fixed values of forces | Qz = 0 kN |
| --- | --- |
| Range of forces | -727,315 kN < N < 728 kN -64,331 kN*m < My < 64,331 kN*m |

Interaction Curves

| Fixed values of forces | My = 0 kN*m |
| --- | --- |
| Range of forces | -727,463 kN < N < 728 kN -300,608 kN < Qz < 300,608 kN |

Interaction Curves

| Fixed values of forces | N = 0 kN |
| --- | --- |
| Range of forces | -64,324 kN*m < My < 64,333 kN*m -300,645 kN < Qz < 300,645 kN |

Report created 2021.02.05 20:46:10 (UTC+02:00) by Kristall (64-bit), version: 21.1.9.9 dated 05.01.2021